| Plant Preparation TECHNICAL GUIDE | TG 02910 |
| --- | --- |

1.	COORDINATION ISSUES:

1.1	Since it is very difficult and expensive to acquire good soil from the Hilo and Kona areas, contact the appropriate Project Coordinator for guidance.

2.	DESIGN ISSUES:  (Not Used)

3.	DRAWING NOTES:  (Not Used)

4.	STANDARD DRAWINGS:  (Not Used)

5.	SPECIFICATION NOTES:

5.1	Topsoil and Planting Soil:.  Include the following requirements whenever topsoil or planting soil is required on a project:

5.1.1	Topsoil or Planting Soil: Soil shall consist of screened (½-inch screen), fertile, friable soil of loamy character and contain a normal quantity of organic matter. Obtain the soil from well-drained, arable land, free from sub-soil, refuse, stumps, roots, heavy or stiff clay, coarse sand, noxious seeds, sticks, brush, litter and other materials which would be detrimental to the proper development of vegetative growth. Soil shall be free from toxic quantities of either acids or alkaline elements.

5.1.2	Soil Analysis: Include provisions for The Contractor to submit to the College of Tropical Agriculture, University of Hawaii, a representative sample(s) (1 pint per sample) of the soil(s) to be used, for analysis. Test for Ph reading, for suitability to support the plant life.

5.1.3	Soil Amendments: Include provisions for the Contractor to provide amendments needed to correct soil deficiencies including phosphates or lime.  Make sure amendments are mixed with the topsoil in the proper proportions before it is spread out in final position. After the amendments are mixed and before planting is allowed, Contractor shall have the soil retested. The Contracting Officer shall be present when soil(s) samples are taken.  Contractor shall correct any deficiencies before proceeding further.

5.1.3.1	Do not allow macadamia nut husk (especially shells) as an amendment in areas to be grassed.

5.1.4	Include provisions for Contractor to pay costs for testing and any required soil amendments needed.

5.1.5	Soil Conditioning: Soil shall be amended by adding soil conditioners such as burnt bagasse, peat moss, redwood chips, or vermiculite. Specify that soil conditioners be thoroughly mixed into the soil at a rate of one part soil conditioner to four parts soil unless a different mixture is desired.

5.1.6	Top Soil: Amendments shall be added to at least the top 6 inches below finished grade.

5.1.6.1	Under areas to be grassed (athletic field, playgrounds) scarify to a depth of 12-6 inches below finished grade until the soil is loose, fine textured and free from stones more than ½ inch in diameter.

6.	GUIDE SPECIFICATION:   (Not Used)

END OF SECTION 02910