| Shingles TECHNICAL GUIDE | TG 07310 |
| --- | --- |

1.	COORDINATION ISSUES: (Not Used)

2.	DESIGN ISSUES: (Not Used)

3.	DRAWING NOTES: (Not Used)

4.	STANDARD DRAWINGS:  (Not Used)

5.	SPECIFICATION NOTES:

5.1	Fasteners

5.1.1	Problem: DAGS has experienced occasional shingle blow-off.

5.1.2	Possible Causes:

5.1.2.1	Installation Deficiencies:

Insufficient number of nails / staples;

Improperly driven nails / staples preventing contact of adhesives or cutting into the shingle,

Shingle edge extending too far past the edge of the eave line, etc.

5.1.2.2	Insufficient Design: Even if shingles were properly installed, a building's height and orientation relative to the wind direction, speed, other buildings and landscape features could also have contributed to or caused the blow-off to occur.

5.1.3	Recommendations: Roofing industry installation standards, the building code, and product literature of the various shingle manufacturers, call for 6 nails per shingle in "high-wind" areas. "High wind areas" are not defined.

5.1.3.1	To minimize shingle blow-off problems, the consultant shall check with the facility's staff to determine whether the project site frequently experiences high-wind conditions or whether shingle blow-off has been a problem in the past.

5.1.3.2	If so, the consultant shall amend their specifications accordingly by specifying additional nails / staples or increasing the shingle's weight.

6.	GUIDE SPECIFICATION:

6.1	Warranty:  (Part 1)

6.1.1	The warranty provisions and number of years for the warrantee by this article shall take precedence over the standard provisions in the GENERAL CONDITIONS.

SPECIFIER’S NOTE: Include the roof components used on the project.

6.1.2	Special Warranty: Roofing Installer and Manufacturer(s), bonded warranty without monetary limitation, in which roof installer and manufacturer(s) agree to repair or replace components of roofing system that fail in materials or workmanship within the specified warranty period.  Failure includes roof leaks, and materials, and adhesion failure due to wind conditions.

6.1.2.1	Special warranty includes roofing membranes and base flashings, [roofing membrane accessories] [roof insulation] [fasteners] [cover boards] [substrate boards] [vapor retarders] [roof pavers] [walkway products] and other components of the roofing system.

6.1.2.2	Warranty Period:  Ten years from the Project Acceptance Date.

6.1.2.3	Wind Conditions: Cover peak wind speeds up to 80 MPH as defined by the Building Code.

6.1.2.4	Warranty shall state the Manufacturer’s acceptance that the roof was installed in accordance with the contract requirements and that the State’s personnel were properly instructed in the maintenance procedures.

6.1.2.5	In the event of a failure State, Roofing Installer and Manufacturer shall mutually agree and determine roof system failures and remedies.

6.1.3	Special Project Warranty: Submit Contractor’s bonded warranty, signed jointly by Roofing Installer covering work of this section, including all components of roof system such as roofing membrane, base flashing, roofing membrane, accessories, roof insulation, fasteners, cover boards, substrate boards, vapor retarders, roof pavers, and walkway products, for the following warranty period and conditions:

6.1.3.1	Warranty Period: Three years from the Project Acceptance Date.

6.1.3.2	Warranty shall cover repairs or replacement of damages to the building and its finishes due to leaks.

6.2	Pre-Installation Meeting (Part 1): The General Contractor, the authorized roofing manufacturers’ representatives or their independent roofing inspectors shall attend a pre-installation meeting.  Include other related trades, such as sheet metal contractor, as applicable.  Confirm the required participants with the Contracting Officer.  Notify participants at least five days prior to meeting.  Intent of the meeting is to review the preparation and installation requirements for the roofing system and to coordinate and schedule the required work.

6.3	Roofing System Manufacturer’s Project Participation (Part 1): General Contractor, Roofing Installer and Roofing System Manufacturer Representative or their independent roofing inspector shall inspect the roof surfaces at the following times:

6.3.1	Prior to the start of the roofing installation,

6.3.2	At the start of the roofing application,

SPECIFIER’S NOTE: Change the number of inspections to suit magnitude and complexity of the project.  A minimum of one inspection is required during the roofing application for roofs not larger than 7,000 square feet with no penetrations and with no roof top equipment mounts.

6.3.3	At least once during the roofing application, unless the Roofing System Manufacturer requires additional inspections for warranty provisions.

END OF SECTION 07310