| Athletic and Recreational Surfaces TECHINICAL GUIDE | TG 02790 |
| --- | --- |

1.	COORDINATION ISSUES: (Not Used)

2.	DESIGN ISSUES: Ensure court surface slopes to drain without pockets of standing water.  Final surface shall be level and without ponding water.  Limit any pockets of ponding to 1/16 inch deep (the thickness of a nickel).

3.	DRAWING NOTES:   (Not Used)

4.	STANDARD DRAWINGS:  (Not Used)

5.	SPECIFICATION NOTES:

5.1	Specification Paragraphs:  As of 03/2003, a complete Guide Specification for Play Surfacing (formerly 02535) is no longer being maintained by DAGS.  Utilize the following specification paragraphs and information as appropriate in the development of the Project Specifications.

6.	GUIDE SPECIFICATION:

6.1	Materials (Part 2): Locally available systems include:

6.1.1	Seal-Master Black Level-Master by Wikel Mfg. Co., Inc.

6.1.2	Laykold Resurfacer by Flintkote.

6.1.3	Huntseal Asphalt Emulsion Park-Top by Western Colloid Products.

6.2	Wear Coat Color: Green.

6.3	Cleaning (Part 3):  New asphalt shall be cured a minimum of 14 days prior to surfacing. New asphalt which becomes dirty shall be well cured before cleaning is attempted.  Existing play surfaces shall be cleaned.  All dirt and loose paint and aggregate shall be removed from the entire area to be surfaced.

6.4	Leveling (Part 3): Court surface shall be leveled in accordance with the following procedure:

6.4.1	The entire area shall be flooded with water and allowed to drain for 20 minutes.

6.4.2	Any areas holding over 1/4" of water shall be marked, dried out, and leveled with a commercially available tennis court mix.

6.4.3	Any areas holding water deep enough to cover a nickel (1/16") and up to 1/4" in depth shall be marked, dried out and leveled with the leveling patch mix. Level in lifts of 1/8" maximum depth each lift and allow to dry completely before applying succeeding lift.

6.4.4	Tack coat shall be applied over newly applied tennis court mix or leveling patch mix prior to Sealer Compound application.

6.5	Tack Coat (Part 3): After all areas are leveled, apply tack coat over entire court.

6.6	Sealer Compound (Part 3)

6.6.1	After the final coat of sealer compound has been applied, rolled and allowed to dry thoroughly, its surface shall be smooth and uniform, showing no evidence of coarse or uneven texture, free of ridges, valleys and tool marks.

6.6.1.1	The completed and rolled surface shall not pond water anywhere to a depth greater than the thickness of a nickel (1/16") when flooded.

6.7	Wear Coat (Part 3)

6.7.1	Wear Coat shall be applied on the clean, dry sealer compound surface.

END OF SECTION 02790