| Tile, Ceramic and Quarry TECHNICAL GUIDE | TG 09300 |
| --- | --- |

1.	COORDINATION ISSUES:

1.1	Coordination with Lath and Plaster: Where mortar set wall tile including Portland cement scratch coat on metal lath, or wire mesh (paper-backed), masonry or concrete is used, include a LATH AND PLASTER SECTION with appropriate specifications.

1.2	Coordination with Provision of Waterproof Membrane: Where a waterproof membrane is required, refer to DAGS Technical Guide TG 07110 - Membrane Waterproofing.

2.	DESIGN ISSUES:

2.1	Expansion Joints:

2.1.1	Refer to Tile Council of America’s "Handbook for Ceramic Tile Installation" and to ANSI A108 Series of tile installation standards for data on expansion joints.  Both require joint locations to be indicated on Drawings.  There is no substitute for showing all joints on Drawings.

2.1.1.1	Locate expansion joints and other sealant-filled joints, including control, contraction, and isolation joints, where indicated during installation of setting materials, mortar beds, and tile.  Do not saw-cut joints after installing tiles.

2.1.1.2	Locate joints in tile surfaces directly above joints in concrete substrates.

2.1.1.3	Tile types have varying water absorption rates. Refer to product manufacturer's recommendations for the recommended spacing of  tile expansion and control joints for each substrate type in your project.

2.2	Floor Level Transitions

2.2.1	Where difference in floor levels exceeds 1/2 inch, a ramp must be used for accessibility for people with disabilities; show ramps on Drawings.

2.3	Tile Repair Projects:

2.3.1	Where existing above-grade toilet/shower facilities are being renovated (e.g. existing floors are being repaired/replaced, partition floor anchors or other devices penetrating the membrane are being removed) the scope of work shall include the repair or replacement of the existing waterproofing membrane as necessary to provide a watertight assembly.

2.4	Floor Tile Installation Method:  Follow Tile Council of America’s Floor Tiling Installation Guide for a minimum “Heavy” service requirement.

3.	DRAWING NOTES:

3.1	Show locations of each type of tile and tile pattern.  Show widths, details, and locations of expansion, contraction, control, and isolation joints in tile substrates and finished tile surfaces. Indicate locations of thresholds.

3.2	Draw details at threshold, wainscot, level transitions, slab control joints, tile expansion joints and at intersections with vertical surfaces.

4.	STANDARD DRAWINGS:  (Not Used)

5.	SPECIFICATION NOTES:

5.1	Specification Paragraphs:  As of 03/2003, a complete Guide Specification for Sections 09310 – Ceramic Tile or 09330 – Quarry Tile DAGS is no longer being maintained by DAGS.  Utilize the following specification paragraphs and information as appropriate in the development of the Project Specifications.

5.2	Performance Requirements: Verify that tile products selected for flooring comply with requirements:

5.1.1	Static Coefficient of Friction:  For tile installed on walkway surfaces, provide products with the following values as determined by testing identical products per ASTM C 1028.

5.1.1.1	Level Surfaces:  Minimum 0.6.

5.1.1.2	Step Treads:  Minimum 0.6.

5.1.1.3	Ramp Surfaces:  Minimum 0.8.

6.	GUIDE SPECIFICATION: (Not Used)

6.1	Submittals (Part 1):

6.1.1	Test Reports:  Submit test reports from an independent laboratory, indicating conformance of the tile to ANSI A137.1 upon request of the Contracting Officer.

6.2	Materials (Part 2):

6.2.1	Ceramic Wall and Floor Tiles:  Standard grade, complying with ANSI A137.1.

6.2.2	Quarry Tile: Quarry tile shall be standard grade, ground 4 sides after firing, with regular smooth surface.

6.2.3	Trim Shapes:  Provide as detailed or as required to achieve a neat complete installation, such as cove base and bullnose.

6.2.4	Setting Materials

6.2.4.1	Dry Set Portland Cement Mortar: ANSI A 118.1.

6.2.4.2	Latex Portland Cement Mortar: ANSI A 118.4.

6.2.4.3	Tile Grout: ANSI A 118.6. Use chemical-resistant, water-cleanable, tile-setting and -grouting epoxy, ANSI A118.3 for quarry tile.

6.2.5	Thresholds

6.2.5.1	General:  Fabricate to sizes and profiles required to provide an wheelchair accessible transition between adjacent floor finishes.

6.2.5.2	Material: Marble Thresholds,  ASTM C 503, with a minimum abrasion resistance of 12 per ASTM C 1353 or ASTM C 241with  a honed finish.

6.2.5.3	Fabrication: Bevel edges at 1:2 slope, aligning lower edge of bevel with adjacent floor finish.  Limit height of bevel to 1/2 inch or less, and finish bevel to match face of threshold.

6.2.6	Mesh: Provide galvanized mesh only.  Rusting of non-galvanized mesh has caused bleed through and discoloration of grout and tile.

6.3	Examination:

6.3.1	Proceeding with tile work will imply acceptance of the substrate condition by the ceramic tile contractor.

6.4	Installation (Part 3):

6.4.1	General: Installation shall be in accordance with ANSI A108.1 - Glazed Wall Tile, Ceramic Mosaic Tile, Quarry Tile and Paver Tile Installation with Portland Cement Mortar and the "Handbook for Ceramic Tile Installation" as published by the Tile Council of America, latest edition.

6.4.2	Expansion and Control Joints: Install expansion and control joints as detailed on the contract drawings.

6.4.3	Thresholds: Install similar to ceramic or quarry tile where shown. Clean as recommended by the manufacturer.

6.4.4	Quality Control: Sound each tile after setting to ensure that they are properly bonded. Replace hollow sounding tiles.

END OF SECTION 09300