| Resilient Flooring TECHNICAL GUIDE | TG 09650 |
| --- | --- |

1.	COORDINATION ISSUES:

1.1	pH and moisture testing with Section 01500 Concrete Moisture Vapor Emission and Alkalinity Testing and Section 03300 Cast-in Placeer Concrete.

2.	DESIGN ISSUES:

2.1	Although marbleized designs are the standard for DAGS projects, the Consultant is not limited.  Consider wear, maintaining, scuff marks, and other conditions when selecting other patterns or solid color tiles.

2.2	Moisture Related Problems:  Due to the lack of moisture and alkali resistance of the current flooring adhesives, there have been a number of blistering and other moisture related problems experienced with resilient tile and sheet vinyl flooring. Therefore, to minimize the occurrence of such problems:

2.2.1	Sheet vinyl flooring shall not be specified unless absolutely necessary.

2.2.2	Specifications shall require testing of concrete floor slabs for bonding and adhesion, moisture and alkali levels in accordance with the floor finish manufacturer's recommendations and instructions. Floor finishes shall not be applied until unsatisfactory conditions have been corrected.

2.3	Floor Finish Problems:  Due to its coarse sandpaper-like finish, the Armstrong Step Master Premium Slip-Retardant Tile is extremely difficult to clean through normal custodial practices in that mopheads and sponges are easily snagged and quickly abraded. In addition, vacuum cleaning equipment (i.e. plates and wheels) are also affected.   Therefore:

2.3.1	This tile shall not be specified on projects constructed under DAGS jurisdiction unless it has been confirmed with the user agency that they have the equipment, staff, time and willingness to adequately maintain the tile in a satisfactory condition.

3.	DRAWING NOTES:

3.1	Information Required:  Show the following on the drawings:

3.1.1	Type, location and layout pattern of floor tile.

3.1.2	Type, location and details of base, edge strips and transitions between resilient tile and other types of flooring.

4.	STANDARD DRAWINGS: (Not Used)

5.	SPECIFICATION NOTES:

5.1	Specification Paragraphs:  As of 03/2003, a complete Guide Specification for Resilient Flooring is no longer being maintained by DAGS.  The Consultant shall utilize the following specification paragraphs and information as appropriate in the development of the Project Specifications.

6.	GUIDE SPECIFICATION:

6.1	Submittals (Part 1):

6.1.1	Manufacturer's cleaning and maintenance data.

6.2	Extra Materials (Part 1) Extra materials are intended for CIP projects and not for the smaller R&M projects.

6.2.1	Make sure extra materials are packaged in their original container and identified with labels describing their contents:

a.	Furnish one (1) box of each type, color, pattern, class, wearing surface and size of tile installed.

b.	Furnish ten (10) lineal feet for each 500 lineal feet or fraction thereof, of each type, color, pattern and size of resilient accessory installed.

6.3	Materials (Part 2)

6.3.1	The standard tile for DAGS Project is - Vinyl composition tile shall be 12 in. x 12 in. x 1/8" thick, conforming to ASTM F1066, Class 2 (through pattern tile), marbleized design with a smooth wearing surface, with a minimum light reflectance of 30%.

6.3.2	Cove base: The rubber or vinyl material shall be free from offensive odor and its color shall be uniform throughout the thickness of the base.

6.3.3	Edging:

a.	Transitions from resilient tile to a different substrate shall be vinyl.

b.	Metal edge strips shall not be used.

6.3.4	Patching and leveling compounds shall be latex-modified, portland cement based formulation unless otherwise required by the flooring manufacturer for the applications indicated. Under no circumstance shall Gypsum based leveling and patching compounds be used.

6.4	Preparation of Subfloors  (Part 3)   If underlayment is required over concrete or wood floors, describe where this is to be laid and specify it completely in this subsection. Omit all references to wood subfloor if it is inapplicable to your job. If wood subfloor is used, its preparation such as power sanding and filling of cracks shall be specified under the CARPENTRY SECTION.

6.5	Project Conditions (Part 3)

6.5.1	Flooring materials and the spaces to receive flooring materials shall be conditioned in accordance with the flooring manufacturer's recommendation and instructions.

6.5.2	Provide adequate ventilation to remove moisture and fumes from the areas where floor tiles are being installed.

6.6	Testing (Part 3)

6.6.1	Flooring materials shall not be installed over concrete slabs until the slabs have cured and are sufficiently dry.

6.6.2	After cleaning, ensusre concrete slabs are tested for alkalinity, moisture and adhesive bond as recommended by the flooring material manufacturer in accordance with section 01450 Moisture Vapor Emission and Alkalinity Testing. Floor tile installation shall not proceed until unsatisfactory conditions have been corrected.

6.6.3	If testing shows the moisture content or alkalinity is not within the Floor Manufacturer’s requirement, Contractor shall provide remedial work, including a floor scaling system or other acceptable means to assure compliance with the Floor Manufacturer’s requirements, in accordance with Section 03300 Cast-in Place Concrete.

6.7	Installation of Materials (Part 3)

6.7.1	Flooring and cove base shall continue, respectively, under and behind removable and/or portable cabinets, cases, etc. Flooring shall continue into closets where the floor of the closets and adjacent floor are at the same level. Installation shall not begin until the work of other trades, including painting, has been completed.

6.7.2	Cove base shall be applied onto thoroughly-dried walls with cove base adhesive only. Because of the thermoplastic character of vinyl base, care shall be taken not to stretch it during installation since it will shrink and leave a gap at joints. The top and bottom edges shall be in firm contact with the wall and floor.  Pre-molded interior and exterior corners shall be used unless otherwise approved by the Contracting Officer. If corners are formed on the job, the wrap around from the corner shall be not less than 12 inches long. Otherwise, the cove base shall be continuous around the corners.

6.8	Cleaning and Protection (Part 3)

6.8.1	Spots of adhesive shall be removed immediately as work progresses. Floor shall not be washed or waxed until the adhesive has completely set, and in no case until after the minimum length of time recommended by the manufacturer has elapsed. The flooring shall be cleaned with a neutral cleaner as recommended by the manufacturer and then damp-mopped with clear water. Flooding of the floor is not permitted. When the floor is dry, 2 coats of an approved non-slip wax shall be applied with a clean lambs wool mop. Each coat shall be buffed thoroughly when dry with a weighted rotary electric floor polishing machine. After polishing, the Contractor shall be responsible for protecting the flooring until acceptance of the project.

END OF SECTION 09650